## Slide 1
Microwave-Assisted Spray Carbonation of mineral slurries: Influence of
Injection Mode and Reaction Parameters on Carbonate Formation
Andrea Erroi, Andrea Rusconi, Marcello Campione
Department of Environmental and Earth Sciences,
University of Milano-Bicocca, Piazza della Scienza 4, Milano, Italy
SelSim2026 Symposium on microscopic characterization of the solid/liquid interface

## Slide 2
THE PROBLEM OF CO2
Global warming: a rise in the Earth’s average temperature
Extreme weather events: heatwaves, droughts, floods and storms
The melting of the polar ice caps and the resulting rise in sea levels
Ecosystem disruption, loss of biodiversity, ocean acidification

## Slide 3
THE PROBLEM OF CO2
Energy production from fossil fuels
Transport: cars, lorries, aeroplanes and ships
Steel manufacturers, cement producers, chemical industry
Buildings: heating and cooling systems
Agriculture and farming

## Slide 4
HOW TO CAPTURE CO2
In aqueous solution:
CO2 (g) + H2O (l)  CO2 (aq)
CO2 (aq) + H2O (l)  H2CO3 (aq)
H2CO3 (aq)  HCO3- (aq) + H+ (aq)
HCO3- (aq)  CO3-2 (aq) + H+ (aq)
A basic solution helps CO2 to dissolve, as it shifts the equilibrium, causing the formation of HCO3- and CO3-2 ions from CO2 (aq)
In an aqueous environment, CO2 dissolves in water
A small proportion of the dissolved CO2 undergoes hydration to form H2CO3
The equilibrium is heavily shifted to the left: only a small fraction of the dissolved CO2 is present as true carbonic acid
Carbonic acid can subsequently dissociate and form HCO3- and CO3-2 ions
In basic solution:
CO2 (g) + H2O (l)  CO2 (aq)
CO2 (aq) + OH- (aq)  HCO3- (aq)
HCO3- (aq)  CO3-2 (aq) + H+ (aq)

## Slide 5
HOW TO CAPTURE CO2
Ca(OH)2 (aq) + CO2 (g)  CaCO3 (s) + H2O (l)
Layered brucite-type structure
Ca2+ atom is octahedrally coordinated by six hydroxyl groups OH- to give CaO6 octahedra that share edges to form a two-dimensional sheet
The individual layers are held together by weak van der Waals forces and residual hydrogen bonds
Portlandite is highly soluble in water and thus releases OH- ions, which promote the dissolution of CO2, and Ca2+ ions, which form carbonates
Ca(OH)2 (aq)  Ca2+ (aq) + OH- (aq)
CO2 (aq) + OH- (aq)  HCO3- (aq)
HCO3- (aq)  CO3-2 (aq) + H+ (aq)
Ca2+ (aq) + CO3-2 (aq)  CaCO3 (s)

## Slide 6
HOW TO CAPTURE CO2
Ca(OH)2 (aq) + CO2 (g)  CaCO3 (s) + H2O (l)
the lamellar nature allows water molecules and CO2 to easily penetrate between the layers
A layer of water adsorbed on the crystal surface acts as an ionization medium, catalysing the transformation of CO2 into carbonic acid (H2CO3) and facilitating the ion exchange
The coordination octagon of calcium is distorted by polyhedral rearrangement to accommodate the planar carbonate anion, changing from the layered structure of portlandite to the rhombohedral structure of calcite/aragonite
Lattice energy of CaCO3 is significantly more stable than that of portlandite

## Slide 7
CLASSICAL
CARBONATION SET-UP
The carbonation of Portlandite is a spontaneous reaction that also takes place at room temperature
However, to increase the reaction rate, hydrothermal synthesis in sealed reactors is used
Temperature:
Increase ion mobility
Increase solubility of Ca(OH)2
Accelerates the nucleation and growth of carbonate crystals
Increase the partial pressure of CO2
Reduction of the synthesis duration
Control of polymorphs
Microwaves:
Efficient and faster heating
Minimisation of temperature gradients
Better temperature control

## Slide 8
EXPERIMENTAL SET-UP
Flux regolator
CO2 tank
Slurry injection system (spray/dropping)
CO2 tube
Slurry reservoir
Slurry injection system (spray/dropping)
CO2 tube

## Slide 9
EXPERIMENTAL SET-UP
Portlandite
slurry
Dried
product
25mL/min of Portlandite slurry ([Ca(OH)2] = 23.26g/L)
In ≈1 min slurry fully injected into the chamber
CO2 flow rate ≈9.5 L/min  saturate the MW oven chamber in ≈1 min
MW Power = 800W
4 min in the microwave to dry the slurry completely

## Slide 10
What are the most optimal conditions for carbon capture in this set-up?
CO2 EXPOSURE TIME
EFFECT OF MICROWAVES
SLURRY INJECTION METHOD:
 DROPWISE ADDITION
 SPRAY INJECTION
TEST METHODOLOGY

## Slide 11
RESULTS
effect of CO2 exposure time
In just 4 min, using only CO2, yields ≈70–90%
Spray injection of the slurry results in higher yields after just 2 min  catalytic effect of the spray
Carbonate produced: Calcite
SPRAY
DROP
Portlandite
Calcite
2 min
3 min
4 min
Portlandite
Calcite
2 min
3 min
4 min
Spray
Drop
Portlandite reagent
Portlandite ref.
Calcite

## Slide 12
RESULTS
… Switch ON the microwaves
Spray
Drop
SPRAY
Portlandite
Calcite
2 min
3 min
4 min
Aragonite
Portlandite
Calcite
2 min
3 min
4 min
Aragonite
DROP
In just 3 min, yields >90%
Microwaves lead to higher yields after just 2 min  ≈ 70-80%
Carbonate produced: Calcite and Aragonite
The presence of aragonite is related to microwaves heating
ONLY CO2

## Slide 13
CONCLUSIONS
Spray produces smaller droplets  higher area/volume  promotes the absorption of CO2  increase the yield
Microwaves induce localised heating, inside the drop  increase the reaction kinetics  increase the yield
Aragonite is a metastable form of CaCO3  favored by high temperatures and supersaturation regime  microwaves induces evaporation and supersaturation of the system  increase the % of aragonite phase
Complete conversion to carbonates in <4 minutes
With our system, we have 0.55 g of Portlandite which, under optimal conditions, captures 0.25–0.33 g of CO2 in 4 minutes, producing 0.55–0.7 g of carbonate  In a scale-up system, with 1 kg of Portlandite slurry, we can capture 0.45–0.6 kg of CO2 every 4 min and produce 1–1.3 kg of carbonates

## Slide 14
THANK YOU FOR YOUR ATTENTION

## Slide 15
TEST WITH SYNTHWAVE

## Slide 16
TEST WITH BRUCITE
4 min with CO2 + MW spray
4 min with CO2 + MW drops
Brucite ref.
Brucite reagent

## Slide 17
CONCLUSIONS
A highly dispersed portlandite slurry is injected into the flue gas stream, generating a large gas–liquid interfacial area and promotes CO2 absorption in the droplets.
Simultaneously, microwave irradiation is applied to enhance carbonation kinetics,  increasing CO2 capture efficiency and accelerating the conversion of Ca(OH)2 into CaCO3